## Slide 1: 第二章 半导体中光的传播
Classical Propagation of light in a dense medium
Dielectric constant by the dipole oscillator model
Properties of r:
1) Causality: Kramers-Kronig relationships
2) Dispersion
3) Anisotropy
4) Induced optical anisotropy: The tuning o the n, 
n, 
Notes: 教学重点：n, 之经典对应, kk关系应用，n,  调控
教学难点： K-K 关系之推导；
用PPT讲，稍提前，
用文献补齐 2016.3.1

## Slide 2: Propagation theory
Model:
Light: electromagnetic wave
Atoms and molecule: classical dipole oscillator, n(),  ()
Two propagation parameters:
1. bound electron (atomic) ~
2. vibrational ~
3. free electron ~
Note
Notes: 经典模型，依然是宏微交替，物穷其理。宏观现象的微观对应过程，就是建模，格物的过程，之后，所建模型的还要被拿到宏观世界进行验证。

## Slide 3
Bound electrons (insulators, intrinsic semiconductors)
natural resonant frequency ω0 : infrared / visible / UV spectral regions 1014-1015 Hz
Free electrons (metals, doped insulators)
• 0 = 0 Drude-Lorentz model
Classical model of an atom.
Electrons are bound to the nucleus by springs which determine the natural frequencies
Electron oscillators
(note)
Notes: 1878 Lorentz
1888 EM wave Hertz
Electron found by J. J. Thomson
In 1896, the British physicist J. J. Thomson, with his colleagues John S. Townsend and H. A. Wilson,[13] performed experiments indicating that cathode rays really were unique particles, rather than waves, atoms or molecules as was believed earlier
Bound electrons (insulators, intrinsic semiconductors)
• restoring force for small displacements F = – Ks x
⇒ natural resonant frequency ω0 = (Ks /m)1/2
• ω0 lies in the near infrared / visible / UV spectral regions 1014-1015 Hz
Free electrons (metals, doped insulators)
• Ks = 0 ⇒ ω0 = 0, Free electrons, Ks = 0, 0 = 0
Drude-Lorentz model

## Slide 4
Molecular physics
IR absorption at resonant frequency of the vibrational modes
Ionic crystals
IR absorption at frequency of optically-active lattice vibrations i.e. the transverse optic (TO) phonons
Vibrational oscillators
Classical model of a polar molecule (an ionic optical medium)
Vibrational oscillators

## Slide 5
Refractive index：
Phase lag
Light emission：
“Hertzian dipoles”
Absorption：resonance
P =N p
D = ε0 E + P = εrε0 E
Dipole oscillators (review)
Note
Notes: Refractive index
If   0,, non-resonant, transparent The oscillators follow the driving wave, but with a phase lag. The phase lag accumulates through the medium and retards the propagation of the wave front, leading to smaller velocity than in free space (v =c / n). -- the origin of n
Light emission
• natural oscillations at ω0
cause radiation at ω0
• “Hertzian dipoles”
Absorption
• light frequency = ω0
• resonance phenomenon
• atoms absorb energy from
the light beam

## Slide 6
Lorentz oscillator (detailed)
Light wave will drive oscillations at its own Frequency
Notes: 本振，简谐振动

## Slide 7
The macroscopic polarization of medium P:
The electric displacement D:
Lorentz oscillator

## Slide 8
Lorentz oscillator
偶
奇
低频
高频

## Slide 9
Lorentz oscillator
低频
高频
按五参量，四常量（可绘图）

## Slide 10
Lorentz oscillator
with
ω0 = 100 THz
γ = 5 THz
εst = 12.1
ε∞ = 10
o  间反常色散
absorption at ω0
• FWHM = γ
Lorentz oscillators










Notes: 

## Slide 11: Example: atomic absorption line
• sodium gas, N = 1×1017 m–3 (low density  n0 1)
• D2 line at 589.0 nm, hyperfine component with FWHM = 100 MHz

## Slide 12
Resonant frequencies:
phonons IR/ valence electrons vis/UV core electrons X-ray
• fj = oscillator strength
• classical theory ⇒ fj = 1
• quantum theory ⇒ fj determined by transition probability,
Multiple resonances










Notes: 
 ？
n<1, 相速
钻头
相速，群速，能量传递速度，信号速度

## Slide 13
Experimental: SiO2
Transparency
band gap
phonon
Notes: 完成“宏微交替”的过程！但尚未“物穷其理”

## Slide 14: Appendix: Local field corrections
local fieldapplied field in dense medium
Clausius Mossotti relationship
Lorentz correction:
in cubic crystal

## Slide 15
The Kramers-Kronig relationships
not independent:
the law of causality + complex number analysis
P indicates that the principal part of the integral should be taken. The K-K relationships allow to calculate n and , and vice versa.
For semiconductor
() ，
n, 
Notes: The refractive index and the absorption coefficient are not independent parameters but are related to each other. If invoking the law of causality and apply complex number analysis, we can derive general relationships between the real and imaginary parts of the refractive index as follows:
上式到下式的过程首先是积分区间的变换（数学）接着直接加上低频（直流）电导（卡帕项）
() ，complete for light propagation
Q1: since =0 in visible range， why Refractive index of Glass 1?
In other words, since =0 in visible range,
then the refractive index of Glass should be 1 in visible range?
Q2: kk implication: common sense
phase Vs absorption
原始文献：Kramers kronig

## Slide 16: Causality and dispersion
Phys. Rev. 104, 6, 1760 （1956）
P60, Electrodynamics of Solids
Dressel and Grűner, Cambridge

## Slide 17
随堂练习
P46
Example：
Calculate the refractive index at low frequency on the assumption that 0 >> .
Solution:
姓名：
20190225

## Slide 18: Application Example of K-K relations
• Refractive index (n) and absorption (κ) are the real and imaginary parts of the same function:
ñ = n+iκ ， thus,
• Absorption and refraction are related to each other by the Kramers–Kronig relationships
Explain the Figure

## Slide 19
将 代入，可得
K-K关系的实验应用
PbTe： Gibson 1961， n=5.8
测量 n0=5.35
P 26 半导体光学 2nd 沈学础
93
(a)碲(Te)晶体的光电导谱实验数据;
(b)虚线为使用KK关系计算的r()谱； 实线为实验测得的r()谱

## Slide 20
Dispersion
This dispersion mainly originates from the interband absorption in the UV and the vibrational absorption in IR
• Group velocity
dispersion (GVD)
• GVD determines
pulse spreading
in optical fibers
• GVD = 0 near 1300 nm
Notes: The Lorentz model indicates that GVD is positive below an absorption line and negative above it. There is a region of zero GVD around 1.3 m in silica. So short pulses can be transmitted down the silica fibre with negligible temporal broadening at this wavelength.
光脉冲展宽：空域，时域

## Slide 21: Dispersive prisms
• NORMAL dispersion: n increase with frequency
• ANOMALOUS dispersion: occurs near resonance lines
Dispersion of light by a prism
Notes: • NORMAL dispersion: n increase with frequency
• ANOMALOUS dispersion: occurs near resonance lines
Dispersive prisms

## Slide 22: Optical anisotropy
Birefringence caused by difference of dielectric constants
(and hence refractive index) along the different crystal axes.

## Slide 24: Double refraction (Birefringence)

## Slide 25: Double refraction in calcite
Birefringence (optical anisotropy) : refractive index depends on the direction of the polarization vector relative to the crystal axes
Birefringent crystals
such as calcite
(Iceland Spar)
separate orthogonal
light polarizations
into the
o(rdinary) and
e(xtraordinary) rays
入射面，主截面，负折射

## Slide 26: Polarizing beams splitters
Critical angle: sinc = 1/n
Calcite: no = 1.658, c = 37.1°; ne = 1.486, c = 42.3°
Hence choose 37.1 ≤  ≤ 42.3°

## Slide 27: Wave plates
Half wave plate: =
Quarter wave plate: =/2

## Slide 28: Induced birefringence
• Isotropic materials are non-birefringent
• Induce birefringence n with strain or electric field
• Hence photo-elastic and electro-optic effects
• Kerr effect (quadratic electro-optic effect) observed in
all materials, including liquids and glass:
Δn =KE2; K = Kerr constant
• Hence Kerr cells (see Fig. 11.8)
• Contrast with linear electro-optic effect (Pockels effect)
observed only in anisotropic crystals

## Slide 29: Chirality
• Optical properties different for left or right circularly polarized
light due to chirality (helicity) of molecules or crystal
structure
• Circular dichroism: different absorption for left or right
circular light
• Optical activity: different refractive index for left or right
circular light.
• Optical activity causes rotation of linear light: Examples:
dextrose, laevulose (fructose) [latin dexter, laevus]
amino acid

## Slide 30: Magneto-optics: The Faraday effect
• Induce chirality in non-chiral materials with a magnetic
field
• magnetic circular dichrosim in absorbing materials
• Faraday effect in transparent materials: rotation of linear
polarization by magnetic field
θ = V B d ;
V = Verdet coefficient

## Slide 31: n, 调控
Kerr effect 1875,
Pockels effect 1893
3. Si 中等离子体色散效应,
4. 折射率的热光效应（Si）
5.手征与圆偏振调控
Modulator
Notes: Kerr effect 1875, Scottish physicist
Pockels effect 1893 German physicist

## Slide 32: MOS optical waveguide/Modulator
Carrier injection p-i-n diode in forward bias
Strong effect (many carriers)
Slow effect (~1GHz)
Carrier depletion
p-n diode in reverse bias Weaker effect → hence device length large
Fast effect (>40GHz)
Change of free carrier density alters Si refractive index & absorption
Intel 04 Nature
Notes: 余金中 半导体光子学 P261 有推导。其中用到1）对自由载流子，0->0; 2）透明区 ->0

## Slide 33: 课堂总结
Notes: 经典传播模型
K－K关系
n,  调控

## Slide 34
A certain material has a single absorption band which runs from photon energy E1 to E2. On the assumption that the absorption coefficient has a constant value 0 within the band, and is zero elsewhere, use the K-K relationship to show that the refractive index for a photon energy E below E1 is given by
Note：
also by use of the relationship of  and E and that of  and 
作业
Exercise 2.12 M. Fox 2nd, P59

## Slide 35
A damped oscillator with mass, natural frequency 0, and damping constant  is being driven by a force of amplitude F0 and frequency . The equation of motion for the displacement x of the oscillator is as show in the following equation. Now,
What is the phase of x relative to the phase of the driving force?
作业（选作）
M.Fox, 1st , Ex 2.2, 可观看视频后直接写出答案。

## Slide 36
附：K-K关系之证明
P56, Electrodynamics of Solids
Dressel and Grűner, Cambridge

## Slide 37
Kramers－Kronig relations
Linear response：
Local approximation:
response function
External perturbation
The law of causality and effect:
Non local effect
P. C. Martin,
Phys Rev 161,143(1967)

## Slide 38: Kramers－Kronig relations
In Fourier space:
凑

## Slide 39
Kramers－Kronig dispersion relationships
色散：实部与虚部之间的内在关系，即K-K变换关系。
In complex frequency plane for mathematical reason
For
(The law of causality and effect)
when 2

## Slide 40
  ii. Convergent ：when   时, G ( ) 0，
  G ( )/在上半复平面内的无限半圆周上积分为0；
  响应函数性质：Lorentz模型
在  的复平面
iii. Parity: G*(-) = G()
对实的，复G()的实部为偶函数，虚部为奇函数，如极化：
fi---振子强度
  i. Analytic ：在上半复平面包括实轴解析

## Slide 41
C
响应函数实部和虚部的关系
（Cauchy’s theorem）
在 的复平面内，采用的积分回路C
 





note
留数定理

## Slide 42
响应函数K-K变换

## Slide 43: 交流电导中的K-K关系
是响应函数

## Slide 44: 介电函数中的KK关系
极化率：
是响应函数
Notes: 接下来通过积分域的数学变换 和 低频直流电导的直接引入，把上式修正以适合半导体的情况。Go on

## Slide 45
积分域变换（数学）
若奇函, 此项留；
 2()是奇函;
 1()是偶函;
若偶函, 此项留

## Slide 46
积分域变换（数学）
2()是奇函；1()是偶函
0, 2 0
对金属和半导体:
传导电导
原式仅适用于绝缘体
note
Notes: 待证 ？？？

## Slide 47: 关系 （备用）
n, 
1, 2
1, 2
Local Approximation
再由 Eqn 7.15知
The relationship
附录
Note
比对下划线： ；
Notes: Note:
1 in phase term, 同步，对电场的响应
2 out of phase, 感生项， 对电场响应

## Slide 48: 关系(备用)
P 23 半导体光学 2nd 沈学础

## Slide 49: 2的修正
原仅适用于绝缘体
适用至半导体
半导体光学
2nd 沈学础
2

## Slide 50: 介电常数中的KK关系

## Slide 51
折射率中的KK变换
当  时,
收敛；解析性和奇偶性同
故 （n-1）+i的实虚部满足KK关系
已知

## Slide 52: 折射率中的KK关系

（证毕）

## Slide 53
http://nobelprize.org/nobel_prizes/physics/laureates/2009/phyadv09.pdf
SiO2 optical fiber
95%
80%
衰减

## Slide 54
光吸收系数:
半导体中光的吸收谱 (概念)
自由载流子吸收
自由载流子吸收
附