## Slide 1: Solar cell efficiency

## Slide 2: 第三章 半导体带间光吸收
Interband absorption
The transition rate for direct absorption
Band edge absorption for direct band gap
Band edge absorption for indirect band gap
Absorption beyond band gap
Absorption measurement at different conditions
Photodetectors & solar cells
Notes: 章节结构：fundamental-> device；(interband) absorption->photodector and solar cell.
Fundamental: rate -> direct gap; indirect gap; absorption beyond band gapmeasurement at different conditions (ltuning);

## Slide 3: Interband absorption
光吸收系数:

## Slide 4: Interband absorption
• Photon excites electron
from filled valence to empty conduction band
• Fundamental
absorption edge at Eg
• Process creates an
electron–hole pair
●
●●

## Slide 5: Direct absorption
• kphoton = 2π/λ ~ 107 m–1 negligible compared to B.Z. size π/a ~ 1011 m–1
• Transitions appear as vertical lines on E – k diagrams for direct band gap
• Phonon needed to conserve momentum for indirect gap materials, therefore low probability
C.B. minimum
at k = 0

## Slide 6: 吸收系数与跃迁速率
x
Light
S=phc/nR, 光通量W/m2
参考 叶良修，半导体物理（上）P506
wi-j: 跃迁速率
S
Notes: 跃迁速率：单位体积单位时间吸收跃迁的次数（几率和）,

## Slide 7: Direct transition rate
空间部分
Fermi’s golden rule
附录1
少了啥？
Notes: Fermi’s golden rule：0t 时间内,常微扰或周期微扰，t 足够长，周期微扰使得跃迁矩阵元中的不含时间部分，平均的后果，故，是单位时间的跃迁数，就跃迁（速）率。
单位时间，单位体积的跃迁几率－速率
Semi-classical：
Wavevector conservation ; “vertical transitions”

## Slide 8: Absorption @ direct band edge
Joint DOS
附录2
含宇称等选择定则
Notes: Absorption spectra characteristics：Strong; Continuous; Broad

## Slide 9: Atomic physics of semiconductors
• Four valence electrons per atom: Group IV (C, Si, Ge),
• III-V compounds (GaAs, InAs, InSb, InP, GaN ….)
• II-VI compounds (ZnS, ZnSe, CdSe, HgTe, …. )
• V.B. → C.B. is p → s, hence allowed transition
Ge: 4s24p2
Si: 3s23p2
sp hybridization
选择定则

## Slide 10: GaAs band structure
• Direct gap at 1.5 eV (0 K)
• Very important
optoelectronic material
• Strong absorption for ħω > Eg
Camel back; X valley
Symmetry points
Γ 000
X 100
010
001
K 110
L 111
fcc lattice Brillouin zone

## Slide 11: InP band structure
http://www.ioffe.ru/SVA/NSM/Semicond/InP/bandstr.html
Direct gap @
Eg=1.34 eV
Long wavelength laser material

## Slide 12: Four-band model
• Simplified band
•Parabolic appr. E~k
valid near k = 0
• Split-off hole
transitions also possible
Notes: structure first proposed by Kane (1957)

## Slide 13: Examples for direct band edge absorption
deviations from e.g. due to phonon absorption or non-parabolicity of the bands
(a) InSb at 5 K
(b) GaAs at 300 K

## Slide 14: Indirect absorption
• Phonon needed to conserve momentum for indirect gap materials, therefore low probability: kf=ki+kphtnq
Wavevector conservation

## Slide 15: Direct versus indirect absorption
• Direct absorption is
much stronger than
indirect absorption
•Silicon has indirect gap at 1.1 eV
• GaAs has direct gap at
1.4 eV
Edge absorption tells..

## Slide 16: Edge absorption tells..
Ge, Si, GaAs, AlGaN基本吸收

## Slide 17: Germanium band structure
• Indirect gap
at 0.66 eV
• Direct gap
at 0.80 eV

## Slide 18: Germanium band edge absorption
• indirect absorption: α ∝ (ħω – Egind ± ħΩphonon )2
• direct absorption: α ∝ (ħω – Egdir )½
Egind = 0.66 eV
Egdir = 0.80 eV
Application !!
α2 (1012 m−2)
Notes: Ge: 吸收特别处：两个带边离不远

## Slide 19: 随堂练习
Exercise 3.7 (p93)
Use the data given in Fig.3.11 (p81) to estimate the absorption coefficient of Ge at 1200 nm at room temperature.

## Slide 20: Silicon absorption above band edge
• Indirect at 1.1 eV
• density of states g(E) ∝ 2 g(k) (dE/dk)–1 ， E
• Critical points (van Hove singularities) whenever dE/dk = 0
@E1 (3.2 eV) & E2 (4.3 eV)
• occurs when conduction and valence bands are parallel to each other: “Parallel band effect”
Silicon band structure
Notes: 4 带边以上的吸收 MIT P28, 黄昆 P215
dE/dk=0 DOS=g(k)/(dE/dK) 
20

## Slide 21: Absorption spectroscopy measurement
Measure transmission coefficient;
Si arrayed
detectors
2. Measure reflectivity spectra R (ħ)
measurements@ different E, B, T, Pl, l:
Notes: Self-consistent fitting of the reflectivity spectra using the Kramers-Kronig formula.

## Slide 22: The Franz-Keldysh effect
Electro-optic effect
The electric field modulated optical constants (n,).
(K-K relationship).
Electroreflectance
The reflectivity can be changed due to modulated optical constants (n,).
Two main effects on band edge absorption by application of an external electric field E（note）
测量条件对吸收的影响
Notes: German physicist Walter Franz and Russian physicist Leonid Keldysh 1958；Germany; Ruassian

## Slide 23: Band in a strong electric field
For the Franz-Keldysh effect

## Slide 24: Example for the Franz-Keldysh effect
R. Williams Physics Rev. 117, 1487 (1960)

## Slide 25: Modulator principles
Electro-Optical
Franz-Keldysh
Pokels, Kerr

## Slide 26: Magneto absorption in germanium
• direct gap at 0.80 eV
• B-Field quantizes motion in direction perpendicular to B
• Landau level absorption
when
ħω = Eg + (n+½) ħ ωc
ωc = eB / me
(cyclotron frequency)
Two consequences:
The absorption edge shifts by heBZ/2;
Equally spaced peaks in the spectrum.

## Slide 27: Landau level
B
Quantum:
ħω = Eg + (n+½) ħ ωc
Suppose B direct is along z
Classic:
ω = eB/m0

## Slide 28: Spin injection in quantum wells
Selection rules
σ+: Δm = +1
σ−: Δm = −1
No crossing
LS 耦合跃迁Selection rules：
ΔS = 0; ΔL = 0,1; ΔJ = 0,1; (J=0J=0 除外)

## Slide 29: Spin injection in quantum wells
The parity different.
 j = 0 ，1 (Total angular momentum).
 l =  1.
 ms = 0. (Spin quantum numbers never change).
Electric-dipole transition: high transition rate, short radiative lifetime(10-9– 10-8 s)

## Slide 30: (Heavily) Doping
Burstein-Moss
Effect

## Slide 31: Photodetectors
Quantum Efficiency
Responsibility A/W
Direct bandgap
Reverse bias
Photoconductive Mode; Photovoltaic Mode
Response time
Noise
Eg, T…

## Slide 32: Photodetectors
• Embed absorbing region within
p-n junction to form p-i-n diode
• Apply reverse bias V0
• Electric field ε = (Vbi – V0) / li
• Vbi = built-in voltage ≈ Eg / e
• Photons absorbed creates e-h pairs in i-region
• Carriers swept out by ε field
into external circuit to generate
photocurrent Ipc
Examples:
• photodiodes
• solar cells (V0 = 0)
ħω > Eg

## Slide 33: p-i-n diodes

## Slide 34: Solar cells (photovoltaics)
• Small gap: large ISC , small VOC
• Large gap: small ISC , large VOC
• Single junction: max efficiency ~30%
• Larger for multi junction

## Slide 35: 课后作业
Exercise (选作)
By referring the figure for the spin injection, prove that the rate for the HH-CB transitions is 3 time as large as that for LH-CB transitions with + light illumination.
Note: Transition matrix element M=<J-1, MJ+1| + | J, MJ >
HH: heavy hole; LH： light hole; CB： conduction band

## Slide 36: 微扰矩阵元
含时微扰矩阵元
t 时刻 出现在m态的几率
含时微扰的波函的展开系数的一般形式，微分积分方程－精确
一级近似，
设上式 an(t)=nm
附录1
（平均）跃迁速率

## Slide 37: Fermi’s golden rule
空间部分, 注意,有的书上是H′/2
0t 时间内,常微扰或周期微扰，t 足够长。
单位时间，单位体积的跃迁几率－速率
量子力学教科书
附录1

## Slide 38: 附录1：含时微扰
空间部分，微扰部分
一个电子（系统）在电磁场中
无微扰
两侧左乘m*(r,t), 并空间积分；
零级波函项左右相抵后：

## Slide 39: 光场微扰算符的形式
电子在电磁场中，非保守力场，用矢势
略去A2项；A，P对易；与无场时的电子能量比较可得微扰。
A与E的关系：
A的具体形式？
p为动量算符-iħ A为电磁场矢势
q 为基本电荷
半经典理论
附录1

## Slide 40: 跃迁动量矩阵元
设微扰是简谐的。
e 矢势单位矢；kp 光波矢 .
略去了光子波矢项
跃迁动量矩阵元
（Vs 偶极跃迁矩阵元）
附录1

## Slide 41: 跃迁动量矩阵元VS偶极跃迁
(Dirac ) Interaction picture
* Fox, P346; 量子力学,曾谨言 4th ed, P165
*
note
附录1

## Slide 42: 跃迁动量矩阵元VS偶极跃迁
e 矢势单位矢, A0常数
E0电场幅值
pe 电子电偶极
附录1

## Slide 43: 偶极跃迁矩阵元
The electron state wave function:
Perturbation:
Dipole moment:
Light wave:
Initial:
Final:
M. Fox, 固体光学性质p52
附录1

## Slide 44: 吸收系数的一般形式
dx
Light
S, 光通量, 入射到单位面积上的光功率,坡因廷矢量的大小
Wfi: 单位体积内单位时间内吸收的入射光子数, 即单位体积吸收入射光的速率
参考 叶良修，半导体物理（上）P506
附录2

## Slide 45: 吸收系数的一般形式的推导
设光场的矢势为A
至此, 只须求出Wfi，即H’fi
矢势表示的poynting 矢量:
推导：曾谨言 量子力学 第四版 II，P431

## Slide 46: 直接禁带
附录2
动量守恒
跃迁动量矩阵元

## Slide 47: 直接禁带基本吸收边
联合态密度:能量守恒+动量守恒
此处的状态数为gCV（ħ ）:
知能带，可求之
附录2

## Slide 48: 态密度函数
取决与E(K )关系，对于自由电子
定义：
。。。。。。。。。。。
。。。。。。。。。。。
。。。。。。。。。。。
。。。。。。。。。。。
。。。。。。。。。。。
。。。。。。。。。。。
。。。。。。。。。。。
。。。。。。。。。。。
。。。。。。。。。。。
。。。。。。。。。。。
附录2
Notes: 48
注：关于态密度的几个关系
m为实空间维度数
V为实空间体积

## Slide 49: 联合态密度
抛物线假设:
附录2

## Slide 50: 简约态密度
美国黑书
附录2

## Slide 51: 直接禁带边吸收系数
附录2

## Slide 52: 直接禁带基本吸收边
容许直接跃迁（项）
禁戒直接跃迁（项）
分别考虑
附录2

## Slide 53: 容许直接禁带跃迁情形
取mr/m0=0.06
=0.2 eV
fCV=1
nR=4
得=1.2x103 cm-1
附录2

## Slide 54: 禁戒直接禁带跃迁情形
因为k 平方项就是动能项(抛物线假设)
附录2